# CS-009 Trimming, Sanding & Finishing

| Doc ID | CS-009 |
| --- | --- |
| Title | Trimming, Sanding & Finishing of Cured Composites |
| Revision | A |
| Status | Draft — pending Lead signature (OUTLINED — complete before first use) |
| Effective date | 2026-07-12 |
| Supersedes | Verbal Dremel training |

Approvals

| Role | Name | Date |
| --- | --- | --- |
| Author | Simon Starbuck (drafted w/ Claude — SN6 Resources) | 2026-07-12 |
| Reviewer | simon (reviewer agent) |  |
| Approver (Composites Lead) |  |  |

Revision history

| Rev | Date | Author | Description of change |
| --- | --- | --- | --- |
| A | 2026-07-12 | Claude | Initial outline |

## 1. Purpose

Cutting and sanding cured CF is where we make our dust (health problem), our edges (quality problem), and — in SN5 — some of our damage: we punctured catch cans sanding thin laminate (2026-05-27), and Dremel work on molds ate heads and marred surfaces. These are the rules for cutting, sanding, and coating cured parts.

## 2. Scope

Cured CF/glass parts: trimming to scribe lines, edge finishing, surface prep for bonding, clear-coating. Waterjet/CNC cutting of flat panels included at outline level.

## 3. References

| Ref | Document | Where |
| --- | --- | --- |
| R1 | DP420 TDS (structural bonding prep) | 04 Datasheets/3m-scotch-weld-epoxy-adhesive-dp420-black.pdf |
| R2 | Catch-can puncture incident | FEB-COMP-PP-001 §PP-05 / minors |
| R3 | CS-002 (sacrificial ply concept), CS-010 (don't sand chasing conductivity) | this series |

## 4. Definitions

Sacrificial ply (88 spread-tow outer layer meant to absorb sanding), trim line (scribe-transferred), keying (abrading for bond).

## 5. Equipment & Materials

Dremel + reinforced cut-off wheels, dust extractor, sandpaper 120→800+, waterjet (Jacobs, via DXF), clear coat (Acrylic Urethane A/B — Lime Line, in stock), DP420 for bonded assemblies.

## 6. Safety

CF dust is the team's worst routine exposure: respirator (P100/dust) + dust extraction ON for any cutting/sanding of cured laminate; long sleeves; gloves — cut CF edges splinter.

Supervision rule (SN5, stands until the lead changes it): no cutting cured carbon without a second trained person present.

Waterjet per Jacobs shop rules.

## 7. Procedure (outline)

Trim only after demould time per resin table (CS-008 §5); mark from scribe lines, tape the cut path (chip control), Dremel with extractor running.

Know the laminate thickness before sanding — check the WO stack. Thin (<3 ply) zones: hand-sand only, count strokes, check often. Machine-sanding thin laminate is how the catch cans died (R2).

Edges: sand 120 → 400; seal exposed edge fibers with a thin resin wipe where cosmetic/sealing matters.

Bond prep: key both faces 120-grit, IPA wipe, DP420 per R1 (2:1, 20 min work life, handling 2 h, full cure 24 h @72 °F).

[ PHOTO: DP420 bond with continuous squeeze-out fillet — the §8 acceptance look ]

Clear coat: per product instructions; record coats on the WO.

Waterjet flat panels: DXF from the requesting subteam through the WO (dashboard lesson — PP-04), confirm rev before cutting.

## 8. Quality checks / acceptance criteria

| Check | Target | Method | Record where |
| --- | --- | --- | --- |
| Trim to scribe | ±1 mm of line | Visual/caliper | WO |
| No sand-through | Sacrificial ply intact / no exposed weave past plan | Visual | WO qualityChecks |
| Bond squeeze-out | Continuous fillet, no starved zones | Visual | WO + photo |

## 9. Records

Trim/sand/bond/coat steps on the WO with operator + date; photos of finished edges and bonds.