# CS-007 Wet Layup & Vacuum Bagging

| Doc ID | CS-007 |
| --- | --- |
| Title | Wet Layup & Vacuum Bagging |
| Revision | B |
| Status | Draft, pending Lead signature (OUTLINED, complete before first use) |
| Effective date | 2026-07-28 |
| Supersedes | Verbal wet-layup training |

Approvals

| Role | Name | Date |
| --- | --- | --- |
| Author | Simon Starbuck (drafted with Claude, SN6 Resources) | 2026-07-12 |
| Reviewer | simon (reviewer agent) |  |
| Approver (Composites Lead) |  |  |

Revision history

| Rev | Date | Author | Description of change |
| --- | --- | --- | --- |
| A | 2026-07-12 | Claude | Initial outline |
| B | 2026-07-28 | Claude | Language pass: fewer em dashes for rhythm variety, no content change. |

## 1. Purpose

Wet layup is our second core process (seat, flat panels, foam-wrapped wing elements). In SN5 the knowledge was verbal plus one Slack SOP; this doc writes it down with the numbers attached.

## 2. Scope

Hand lamination with West System 105, vacuum-bagged, on molds (CS-004-prepped), flat plates, and foam cores (foam-wrapped wing elements). Infusion: CS-006.

## 3. References

| Ref | Document | Where |
| --- | --- | --- |
| R1 | West 105/206 TDS (5:1 by volume; pot life 20–25 min @72 °F; thin-film cure 10–15 h) | 04 Datasheets/WEST_SYSTEM_105_Epoxy_Resin_with_206_Slow_Hardener.pdf |
| R2 | West 105/205 TDS (fast: pot life 9–12 min) | 04 Datasheets/WestSystems-105-205-Epoxy-Resin.pdf |
| R3 | VB160 film, PP180 peel ply, breather | 04 Datasheets/ |
| R4 | CS-002 (stack), CS-004 (mold prep), CS-008 (mixing/exotherm) | this series |
| R5 | Simon’s layup SOP (Slack, 2026-05-30): 105 “big tank, blue label” + 206 “large metal can, red label”, 5:1 | Slack record |

## 4. Definitions

Breather (fluffy bleed cloth — never touching part edges it could bond to), bridging, wet-out, 60:40 fiber:resin target by weight.

## 5. Equipment & Materials

West 105 + 206 (default) or 205 (small parts), calibrated pumps (5:1 by volume, R1) or scale (weight ratios in R1: 5.36:1 for 206), brushes/rollers/squeegees, peel ply, breather, VB160, tacky tape, vacuum pump + trap + gauge.

## 6. Safety

Per West SDS + team rules: nitrile gloves (sensitizer — same warning as CS-004 §6), ventilation, no solvent on skin; exotherm rules per CS-008 (105/205 in a pot gets hot fast). Respirator with A-filter for large overhead/enclosed laminating.

## 7. Procedure (outline — expand with photos on first parts)

- Prerequisites: stack frozen (CS-002 §7.2), mold released (CS-004), cloth cut + weighed.

- Resin math: mix ≈ fiber mass × 0.9 for hand layup. (Yes, that is more than the 60:40 target implies: the squeegee and the breather take the excess out, and the cured part lands near 60:40. Record mixed vs final masses on the WO to tune this factor.)

- Mix per CS-008: 5:1 by volume with the calibrated pumps (R1); one FULL pump stroke each, never partial strokes; pot life 206 @72 °F: 20–25 min per 100 g pot.

- Wet out ply-by-ply per the WO ply table; squeegee each ply until shiny-wet, not swimming.

[PHOTO: correctly wetted ply — uniform sheen, weave visible, no pooling]

- Lay peel ply over the full laminate.

- Lay breather over the peel ply, kept clear of part edges it could bond to.

- Bag with VB160 + tacky tape, adding pleats at corners (CS-006 §7.3 rules apply).

- Pull vacuum to ≥25 inHg; drop test: isolate pump, ≤2 inHg over 10 minutes before walking away. Record readings on the WO.

[PHOTO: bagged wet layup under vacuum, pleats visible, gauge in frame]

- Cure per R1 (206: thin-film solid 10–15 h @72 °F; leave bagged overnight minimum). Record times/masses on the WO.

- Foam-wrapped elements (RW E2–E5 class): same flow over a shaped foam core; watch vacuum crush on light foams — reduce vacuum if the core dents (record the level that worked per part on the WO).

## 8. Quality checks / acceptance criteria

| Check | Target | Method | Record where |
| --- | --- | --- | --- |
| Vacuum | ≥25 inHg; drop ≤2 inHg/10 min | Gauge | WO |
| Wet-out | No white/dry weave visible | Visual per ply | WO |
| Mass | WO target ±10% | Scale | WO qualityChecks |

## 9. Records

Same as CS-006 §9: times, masses, gauge readings, photos into the WO.