# CS-008 Resins, Mixing & Cure Schedules

| Doc ID | CS-008 |
| --- | --- |
| Title | Resins, Mixing & Cure Schedules |
| Revision | B |
| Status | Draft, pending Lead signature (OUTLINED, complete before first use) |
| Effective date | 2026-07-28 |
| Supersedes | Ratio/pot-life tribal knowledge |

Approvals

| Role | Name | Date |
| --- | --- | --- |
| Author | Simon Starbuck (drafted with Claude, SN6 Resources) | 2026-07-12 |
| Reviewer | simon (reviewer agent) |  |
| Approver (Composites Lead) |  |  |

Revision history

| Rev | Date | Author | Description of change |
| --- | --- | --- | --- |
| A | 2026-07-12 | Claude | Initial outline, the one-page ratio/cure table every other standard cites |
| B | 2026-07-28 | Claude | Language pass: fewer em dashes for rhythm variety, no content change. |

## 1. Purpose

One table for every resin we stock: ratios, pot lives, cure/demould times, plus the mixing discipline and exotherm rules that apply to all of them. Exists because of soft-spot failures (bad ratios), the first forged-CF part cracking from resin starvation, and a few too many hot cups.

## 2. Scope

All team resin systems. Process-specific use lives in CS-004 (XCR), CS-006 (IN2), CS-007 (West 105).

## 3. References

| Ref | Document | Where |
| --- | --- | --- |
| R1 | IN2 TDS · R2 XCR TDS · R3 West 105/205, /206, /209 TDS | 04 Datasheets/ (see INDEX.md) |
| R4 | SDS for all of the above | 04 Datasheets/ |
| R5 | Forged/Compression Molded CF study (mix math, starvation failure) | SN5 Composites/Documentation/Forged_Compression Molded Carbon Fiber.docx |

## 4. Definitions

Pot life (usable time in the pot at stated mass/temp), gel, demould, full cure, exotherm.

## 5. Equipment & Materials — THE TABLE (verify each against its TDS before signing)

| System | Ratio (by weight) | Pot life | Demould | Full properties | Use |
| --- | --- | --- | --- | --- | --- |
| IN2 + AT30 SLOW | 100:30 | 120–150 min @25 °C | 18–24 h | ≥14 d @25 °C | Infusion default (CS-006) |
| IN2 + AT30 FAST | 100:30 | 10–14 min @25 °C | 6–8 h | ≥14 d | Small infusions only |
| West 105 + 206 SLOW | 5.36:1 (5:1 by volume pumps) | 20–25 min @72 °F | thin-film solid 10–15 h | days | Wet layup default (CS-007) |
| West 105 + 205 FAST | 5.19:1 (5:1 by volume) | 9–12 min @72 °F | 6–8 h | days | Small wet layups, tabs |
| West 105 + 209 | 3.68:1 (3:1 by volume — DIFFERENT pump ratio than 205/206!) | 40–50 min @72 °F (100 g) | thin-film solid 20–24 h | max strength 4–9 d; min temp 70 °F | Hot-day / very large wet layups |
| XCR | 100:41 (2:1 by volume) | 8 min @20 °C (150 g) | 8.5 h initial | ≥14 d @20 °C | Mold sealing (CS-004) |

## 6. Safety — exotherm and sensitization (applies to every system)

- All epoxies here are skin/respiratory sensitizers (R4): nitrile gloves, ventilation, wash skin with soap not solvent, A-filter respirator for long/enclosed sessions.

- Exotherm rules: mix the smallest batch that does the job; pour out of the pot promptly (mass concentrated in a cup accelerates); a warm cup = use immediately or spread thin; a hot/smoking cup = carry outside onto concrete and leave it. Do not bin, do not water-dilute indoors. Nothing goes in the trash until fully cured and cool.

- Never mix off-ratio to “speed up” or “slow down” cure. Blend hardener speeds (same total ratio, per R1/R3) instead; off-ratio = uncured sticky part.

## 7. Procedure (outline)

- Pick the system from §5 by process standard; confirm pot life fits the job + a margin. ⚠ 209 uses 3:1 pumps, not the 5:1 pumps used by 205/206. Check the pump head before stroking; this is the classic wrong-ratio trap.

- Weigh (scale, 1 g) or pump (West, full strokes only); record masses on the WO.

- Mix ≥2 min scraping walls/base; double-pot (transfer + remix, fresh stick) for anything going on a part surface.

- Forged CF mix math (R5): carbon mass ≈ mold volume × 1.4 g/cc; resin ≈ fiber × 1.25. Starving the mix made the first part brittle (failed bend test); don’t eyeball it.

- Cure at ≥20 °C wherever possible; log ambient temp on the WO when it isn’t (cold cures run long — see each TDS).

- Leftovers: spread thin on scrap or leave outside to cure; label per CS-001.

## 8. Quality checks / acceptance criteria

| Check | Target | Method | Record where |
| --- | --- | --- | --- |
| Ratio | Weighed/pumped per §5, recorded | Scale/pump count | WO |
| No soft spots at demould | Fingernail test on flange/trim zone | Manual | WO qualityChecks |

## 9. Records

Batch masses, system + hardener speed, ambient temp, cure duration — on every WO that consumes resin.