# CS-006 Resin Infusion

| Doc ID | CS-006 |
| --- | --- |
| Title | Resin Infusion |
| Revision | B |
| Status | Draft, pending Lead signature |
| Effective date | 2026-07-28 |
| Supersedes | Resin Infusion Beginner Guide (SN5), retained as intro reading; its "30 psi vacuum" figure is wrong (see §7.4) |

Approvals

| Role | Name | Date |
| --- | --- | --- |
| Author | Simon Starbuck (drafted with Claude, SN6 Resources) | 2026-07-12 |
| Reviewer | simon (reviewer agent) — G0 findings incorporated | 2026-07-12 |
| Approver (Composites Lead) |  |  |

Revision history

| Rev | Date | Author | Description of change |
| --- | --- | --- | --- |
| A | 2026-07-12 | Claude | Initial issue. Fixes G0 review findings on the old guide: impossible vacuum number, missing resin trap, no numeric leak-down criterion |
| B | 2026-07-28 | Claude | Language pass: fewer em dashes for rhythm variety, no content change. |

## 1. Purpose

Infusion is our main process for big parts, and in SN5 we ran it on vibes: no numeric leak criterion ("air started leaking in toward the end, hopefully it will turn out okay", #composites, 2026-05-01), an inherited guide asking people to find a physically impossible "30 psi" of vacuum, and no resin trap mentioned anywhere between bag and pump. This doc gives the actual numbers.

## 2. Scope

Resin infusion of CF/glass laminates on sealed tooling-board molds (CS-004) or flat glass/table plates, using the team's IN2/AT30 system. Wet layup: CS-007.

## 3. References

| Ref | Document | Where |
| --- | --- | --- |
| R1 | IN2 Infusion Resin TDS | 04 Datasheets/EC-TDS-IN2-Infusion-Resin.pdf |
| R2 | IN2 + hardener SDS | 04 Datasheets/EC-SDS-IN2-Epoxy-Infusion-Resin-and-Hardener.pdf |
| R3 | VB160 bagging film TDS/SDS | 04 Datasheets/EC-TDS-VB160-Vacuum-Bagging-Film.pdf, EC-SDS-VB160-Vacuum-Bagging-Film.pdf |
| R4 | PP180 peel ply TDS | 04 Datasheets/EC-TDS-PP180-Peel-Ply.pdf |
| R5 | Airtac 2 spray adhesive TDS/SDS | 04 Datasheets/airtac2imp.pdf, airtac2spray.pdf |
| R6 | CS-002 (stack), CS-004 (mold prep), CS-008 (resin handling) | this series |
| R7 | Resin Infusion Beginner Guide (SN5, background reading only) | SN5 Composites/Documentation/Resin Infusion Beginner Guide.docx |

IN2/AT30 key numbers (all from R1):

| Property | Value |
| --- | --- |
| Mix ratio | 100 : 30 resin : hardener by weight (FAST or SLOW hardener, same ratio) |
| Pot life @25 °C | SLOW: 120–150 min · FAST: 10–14 min |
| Gelation @25 °C | SLOW: 8–10 h · FAST: 2–4 h |
| Demould @25 °C | SLOW: 18–24 h · FAST: 6–8 h |
| Full mechanical properties | ≥14 days @25 °C (no oven post-cure available) |
| Hardener choice | SLOW for anything larger than a coupon; FAST only for small parts where you are confident of infusion time |

## 4. Definitions

inHg — inches of mercury, what the team's gauges read for vacuum. Full vacuum at sea level ≈ 29.9 inHg; nothing reads "30 psi of vacuum", since atmospheric pressure is only ~14.7 psi. The old guide's "30 psi" figure was a gauge-scale mix-up; if a gauge shows psi, it is reading something else.

Drop test / leak-down — isolating the bag from the pump and watching the gauge to quantify leaks before committing resin.

Resin trap / catch pot — sealed container between bag outlet and pump that catches over-pulled resin. Without it, the first overlong pull kills the vacuum pump.

Pleats — folds built into the bag with tacky tape so film can reach into corners without bridging or tearing.

Race-tracking — resin finding a fast path (usually along edges) and reaching the outlet before wetting the middle.

## 5. Equipment & Materials

| Item | Spec / product | Source | Notes |
| --- | --- | --- | --- |
| Resin system | IN2 + AT30 SLOW (default) | Easy Composites | R1; order ≥6 weeks ahead (PP-02) |
| Bag film | VB160 | Easy Composites | R3 |
| Peel ply | PP180 (or Sigmatex-supplied) | Easy Composites / Airtech | R4 |
| Flow mesh | Green infusion mesh (or 2-in-1 mesh/peel ply) | Easy Composites / Airtech | Cover the whole part |
| Tacky tape | Sealant/gum tape | Airtech / General Sealants | Keep backing tab on until final placement |
| Spiral wrap ½" + PE tubing ½" | Feed/vacuum lines | Airtech | Watch sharp-cut ends near the bag |
| Resin trap | Team catch pot | RFS | Mandatory in line before the pump |
| Vacuum pump + gauge (inHg) | Team pump | RFS |  |
| Tack spray | Airtac 2 | Airtech | R5; light mist only |
| Digital scale, cups ×2, sticks | 1 g resolution | Consumables | Double-pot mixing (CS-008) |
| Clamp/hose clamp for feed line | — | RFS | The "clamp" in §7.5 |

## 6. Safety

Per R2: IN2 resin and amine hardener are skin/eye irritants and sensitizers.

Gloves: nitrile at all times once resin is out; change after any contamination.

Eyes: safety glasses when mixing and when cutting pressurized lines.

Ventilation: mix and infuse in the ventilated shop area; IN2 vapor pressure is low but sensitization is cumulative.

Airtac 2 (R5): extremely flammable aerosol — no sparks/heat, use in ventilated space, short bursts.

Exotherm: a full mixed pot of IN2 left standing will overheat (CS-008 rules apply: batch sizing, transfer promptly, hot cup → outside on concrete).

Sharp spiral-wrap ends: cut ends pierce gloves and bags alike — tape them.

## 7. Procedure

### 7.1 Prerequisites

Stack frozen and printed on the WO (CS-002 §7.2); mold sealed + released per CS-004 with quality checks passed.

Materials staged: resin on hand ≥ (dry fiber mass × 0.65) × 1.3 (same formula as the mix math in 7.5, rounded up since infusion consumes mesh/line resin too), all consumables cut before any resin is mixed.

Two people minimum for any part bigger than a coupon; one experienced with infusion (unchanged team rule, R7).

### 7.2 Dry stack and consumables

Workspace and mold wiped clean (IPA/microfiber). Cut cloth per the WO ply table; weigh and record total dry fiber mass on the WO.

Lay plies per the WO, tacking with light Airtac 2 mists only where needed (heavy spray inhibits infusion).

Peel ply over the full laminate + flange edges; flow mesh over the entire part stopping 30–50 mm short of the outlet side (the mesh break slows resin at the end and reduces race-tracking through the exit).

Place spiral-wrap feed line along the inlet side on the flange (not on part surface unless the WO says so — print-through), and the outlet spiral toward the catch pot. Max resin travel distance inlet→outlet ≈ 0.5 m (R7 rule of thumb); larger parts need multiple feeds planned on the WO.

[ PHOTO: dry stack with mesh break visible near outlet spiral ]

### 7.3 Bag

Tacky tape around the full perimeter; keep backing on until final placement. ~½ inch spacing from the part edge envelope.

Cut VB160 oversized; add a pleat at every corner and every 300–400 mm of perimeter on curved molds.

Fit through-bag connectors: outlet line → resin trap → pump (never bag → pump directly); inlet line → clamped shut.

### 7.4 Pull vacuum and drop test: the blocker

Pull vacuum. Target on the team gauge: ≥27 inHg (full vacuum is ~29.9 inHg at sea level; RFS altitude is negligible). If the gauge won't pass 25 inHg, hunt leaks now: press tacky tape seams, listen, re-seat pleats and connector bases.

Drop test: close the valve to isolate the pump. The bag must lose ≤1 inHg over 10 minutes. Write start/end readings on the WO.

Fail → keep hunting (seams, pleat folds, connector bases, spiral ends piercing the bag) and re-test. Do not mix resin until the drop test passes. This number is the difference between this standard and SN5's "hopefully it will turn out okay".

⚠ CAUTION: The drop test is cheap. A dry patch in a cured undertray panel is not. No pass, no resin, even at 11 pm with people waiting.

### 7.5 Mix and infuse

Resin mass math: mix ≈ (dry fiber mass × 0.65) × 1.2–1.3. The 0.65 factor covers the laminate (aiming ~60:40 fiber:resin by weight); the 1.2–1.3 multiplier covers mesh/line losses. Round up; starving the infusion mid-pull is unrecoverable, and leftover mixed resin is a known cost (record actual used vs mixed on the WO to tune this).

Mix IN2:AT30 100:30 by weight (R1) per CS-008 (double-pot, ≥2 min). SLOW hardener default: 120–150 min pot life at 25 °C.

Brace the resin cup; submerge the inlet line end fully (a slurping inlet injects the bubbles you just vacuumed out).

With ≥27 inHg confirmed, open the inlet clamp slowly. Watch the flow front: even progress, no race-tracking. Typical small part: 20–30 min; large: longer.

When resin reaches the outlet spiral and the laminate is fully dark/wet: clamp the inlet. Leave the pump running through gel (SN5 practice; the "no 24/7 vacuum" optimization was never validated, revisit only with a deliberate test).

Record on the WO: times (mix, open, full-wet, clamp), resin mixed vs used, gauge readings, anomalies with photos.

[ PHOTO: flow front mid-infusion, even progress across the part ]

### 7.6 Cure and demould

Demould at 18–24 h @25 °C for SLOW (6–8 h FAST) per R1; colder shop = longer, be patient (gel ≠ cured).

Full mechanical properties take ≥14 days (R1) — schedule trimming freely, but no structural/fit loading before then where avoidable.

Demould, label part per CS-001, photograph, weigh, record in WO qualityChecks; hand to CS-009 for trim.

### 7.7 Troubleshooting (the section the old guide promised and never delivered)

| Symptom | Likely cause | Do |
| --- | --- | --- |
| Gauge won't reach 25 inHg | Perimeter leak, connector base, pleat fold | Press seams, re-seat; soapy-water on suspect spots |
| Passes to 27 then creeps down | Micro-leak — spiral end or bag puncture | Patch with tacky tape square; re-drop-test |
| Resin racing along one edge | Race-tracking channel at the flange | Clamp inlet briefly; rely on mesh break; note for next mold (tape a dam) |
| Dry patch far from inlet | Mesh didn't cover; distance >0.5 m | If still wet: emergency second feed. Cured: record as defect, assess vs qualityChecks |
| White/foamy resin at inlet | Bubbles from slurping cup | Re-submerge line; bubbles usually trap in mesh, note location |
| Resin in the trap filling fast | Over-pull past full wet | Clamp inlet earlier next time; trap is doing its job — empty before it nears the pump port |

## 8. Quality checks / acceptance criteria

| Check | Target | Method | Record where |
| --- | --- | --- | --- |
| Vacuum before resin | ≥27 inHg | Gauge | WO |
| Drop test | ≤1 inHg / 10 min | Timed gauge readings | WO (start/end values) |
| Full wet-out | No dry patches visible through bag | Visual at clamp time + after demould | WO qualityChecks + photos |
| Resin usage | Mixed vs used recorded | Scale | WO |
| Part mass | Per WO target ±10% (default) | Scale | WO qualityChecks |

## 9. Records

WO records: drop-test numbers, times, batch masses, hardener speed, gauge log, photos (dry stack, bagged, flow front, demolded), deviations. These records are how the next season learns what 0.5 m really means on our parts.